Hi Mike:

Here are summaries of what we have done so far.

Mar. 26-28

Synchrotron micro X-ray diffraction at SPring-8 Analyzed samples:

C2004,1,44,2   We could obtain diffraction images.

C2054,0,35,6   We could obtain diffraction images.

(These two samples were mounted on glass needles.

They were passed to Tomoki-san after the analyses.) CF12,0,16,3,0  We could obtain diffraction images.

(This sample is a "potted butt".)

Unfortunately, Ohsumi-san has been too busy for retiring matters to have a time to calculate the obtained patterns.

I have analyzed two potted butt samples by FEG-SEM.

FC3,0,2,1,0

Mostly silica-enriched areas, suggesting heavy contamination with silica aerogel.  Only small amounts of Mg and Fe were detected.

(see the attached file)

CF12,0,16,3,0

1.5 micron x 2.5 micron small grain.  EDS showed abundant Si, Al, and K, suggesting that this is a single K-feldspar grain.

(see the attached file)

We have 6 days at KEK for analysis of Stardust samples from May 11 to May 17.

Since we have plenty of time and we hope to analyze several samples.  At SPring-8 we learned that Tomoki- san's sample style (grains mounted on glass needles) is not difficult to analyze.  However, we had a very very difficult time to analyze potted butt samples.  So we hope to have "easily" analyzed samples for our next synchrotron session if some are available.

Best regards,

Takashi