Dear Mike,

This is my report of MINPET results of Stardust samples.

Subject: 3D structures of individual particles removed from aerogel by imaging microtomography.

Samples: 4 particles

particl ID	imaging no.

C2004, 1, 44, 3	060410l

C2054, 0, 35, 6	060410n

C2054, 0, 35, 5	060410j

C2054, 0, 35, 4	060410g

Experiments: Imaging microtomography

Beamline BL47XU of SPring-8

Energy: 8 keV

Voxel size: 0.0425 x 0.0425 x 0.0425 m3

(effective spatial resolution: ~ a few hundreds nm)

Quick summary was appended to Tomoki Nakamura’s file attached in this mail (XRD_CT summary.xls).

Details including images (ppt file) were uploaded at

http://www-bl20.spring8.or.jp/~sp8ct/tmp/stardust_particles

report_final.ppt

Contents of the ppt file:

For each sample,

1st page: CT images (browse image)

2nd page: X-slice images (browse image)

3rd page: Y-slice images (browse image)

4th page: CT value histogram, list of CT values for candidate minerals, and

XRD results by T. Nakamura

5th page: explanation of a CT image

6th page: bird’s eye view images of a particle, size and volume

7th page: bird’s eye view images of a special object

Some movies are also available at

http://www-bl20.spring8.or.jp/~sp8ct/tmp/stardust_particles

060410g.lzh

060410j.lzh

060410l.lzh

060410n.lzh

Summary:

(1) C2004, 1, 44, 3	060410l

Small grains of heavy minerals (kam?: the size must be less than the CT spatial resolution) are embedded in a porous material, which may be aerogel with or without very fine cometary dust samples. Presence of large voids in the porous material (p.6 in the ppt file) shows large-scale vesiculation, such as melting..

(2) C2054, 0, 35, 6	060410n

This particle shows micro-porphyritic texture. If the phenocrysts are olivine, the Mg# estimated from the CT values (linear attenuation coefficients in the CT images) is approximately 0.8 (p.12 in the ppt file). Relatively large kamacite grains are also seen (mode: ~1 vol.%). Small voids are also present (p.13 in the ppt file). The particle is partially covered with a porous material (aerogel + sample?). The particle surface is rounded and any fractured feature is not seen (p.14 in the ppt file).

(3) C2054, 0, 35, 5	060410j

This particle is similar to (1) C2004, 1, 44, 3. Small grains of heavy minerals (kam and Fe-S: the size of some grains must be less than the CT spatial resolution) are embedded in a porous material (aerogel + sample?). Presence of large voids in the porous material (p.20 in the ppt file) shows large-scale vesiculation, such as melting. The porous material has smooth and rough surfaces (p.21 in the ppt file). Fragments of W wires are also seen (pp.16-18 in the ppt file).

(4) C2054, 0, 35, 4	060410g

Crystalline sample. Very small grains of heavy minerals (Fe sulfide or magnetite?: metal is also possible) are present along the grain boundaries of silicates (p.27 in the ppt file). Portions which seem to be mesostasis are also seen (p.27 in the ppt file). If this is mesostasis, this sample has prophyritic texture. Small voids are also present. The particle is partially covered with a porous material (aerogel + sample?). Fractured surface without covering the porous material is also seen (p.29 in the ppt file).

.