Sample Information Sheet

Sample ID: C2054,0,35,24,5

Slice number(s): 19, 21

Sample type (select one):

(1) microtomed slice

(a) epoxy, acrylic or sulfur embedded

Type of analysis performed: TEM (200 keV Philips 320M, 200 keV JEOL 2010), EDX

Analyst: C. H. van der Bogert

State of sample pre-analysis: Good to moderate with some loss of internal fragments (see Figures 1 and 2)

State of sample post-analysis: Unaltered to slightly beam damaged (individual small spots)

Minerals or other phases identified:

- The primary component of this sample was melted and compressed aerogel mixed with melted cometary silicates

- Within the glassy material are numerous metallic and sulfide spherules, including FeS and FeNiS compounds (see Figure 3).

Contaminant phases identified: This sample is primarily composed of heavily melted cometary material mixed with melted and compressed aerogel.

Figure 1. Bright-field TEM photomicrograph mosaic of sample C2054,0,35,24,5, slice #19.

Figure 2. Bright-field TEM photomicrograph mosaic of sample C2054,0,35,24,5, slice #21.

Figure 3a. Bright-field TEM photomicrograph of sample C2054,0,35,24,5, slice #21 (27,500x). The dark phase in the middle of the image is the location of the EDX spectum in Figure 3b.

Figure 3b. EDX spectrum showing a FeNiS composition with strong  Si and O signals, due to surrounding aerogel and melted cometary silicates (the probable origin of the Mg signal in the first spectrum). The first spectrum was not quite centered on the black phase; the second spectrum was better centered. Cu and C signals are from the sample grid.

References:

van der Bogert C. H., Stephan T. and Jessberger E. K. (2009) Separation of primary amorphous silicates and capture-related glasses in Stardust cometary samples. Lunar Planet. Sci. 40, #2404.

van der Bogert C. H., Stephan T. and Jessberger E. K. (2008) Capture-processing of Stardust cometary particles: Comparisons of melted and unmelted particles from Type B impact tracks. Eur. Planet. Sci. 3, #546.

van der Bogert C. H. and Stephan T. (2008) Comparison of capture-melted and unmelted Stardust cometary particles: Preliminary TEM analyses. Lunar Planet. Sci. 39, #1732.