Track 57 (Febo):  C2009,2,57

Type: B

Length:  >1.4 mm

Sample type:  microtomed slices embedded in acrylic

Analysis method:  TEM

State of samples:  variable surface carbon contamination from electron beam, possible damage to internal crystalline structures

Mineralogy and apparent grain sizes

Terminal particle (8 um) – Fragment 1

Pyrrhotite (4 um)

Attached to pyrrhotite are ~1um crystals of Fo97 and En98 and fine-grained ~chondritic debris (Fe-sulfides, silicate glass, kosmochloric diopside and carbonaceous material)

Isotopic composition of fine-grained C phases:  (15N = 480 – 640 ‰, (13C = ~ 0 to – 75 ‰

Fragment from bulb area (1 um)

Fo99.2 (olivine structure confirmed by ED)

Moderate amount of melt.

Other minor/trace minerals observed:

None