Track 58 (Noni):  C2009,3,58

Type: A

Length:  0.29 mm

Sample type:  microtomed slices embedded in acrylic

Analysis method:  TEM

State of samples:  variable surface carbon contamination from electron beam, possible damage to internal crystalline structures

Mineralogy and apparent grain sizes

Terminal particle (< 5 um) – Fragment 1

Core of Fe oxides and Ni oxides with surrounding shell of submicron ~Fo90-95, Mg+Al silicate glass and kosmochloric diopside.  Electron DPs consistent with olivine and diopside atomic structures.

Other minor/trace minerals observed:

None