Track 59 (Naomi):  C2009,4,59

Type: A

Length:  0.35 mm

Sample type:  microtomed slices embedded in acrylic

Analysis method:  TEM

State of samples:  variable surface carbon contamination from electron beam, possible damage to internal crystalline structures

Mineralogy and apparent grain sizes

Terminal particle (> 3 um) – Fragment 1

Fe-sulfide:  mixture of pentlandite, pyrrhotite and a Ni-rich sulfide (heazlewoodite) with abundant interstitial pure SiO2 glass (aerogel melt).

Fragment 2

Fe-sulfide:  mixture of pentlandite, pyrrhotite and a Ni-rich sulfide (heazlewoodite) with abundant interstitial pure SiO2 glass (aerogel melt).

Minor/trace minerals observed:

None