Track 61 (Allie):  C2009,6,61

Type: A

Length:  1.6 mm

Sample type:  microtomed slices embedded in acrylic

Analysis method:  TEM

State of samples:  variable surface carbon contamination from electron beam, possible damage to internal crystalline structures

Mineralogy and apparent grain sizes

Terminal particle ( 5 um) – Fragment 1

Al+Cr+Fe silicate glass, Fo99+

Significant Fe oxide present on exterior of fragment (laboratory oxidation?)

Minor/trace minerals observed:

None