Sample Information Sheet

Sample ID: C2013N

Sample type (select one):

(6) foil

Type of analysis performed: 	SEM search for impact craters; C, N, O-, and S-isotopic compositions (NanoSIMS) and EDX in large crater

State of sample pre-analysis: good

State of sample post-analysis (select one): largely consumed (large crater)

Minerals or other phases identified:

- a. elemental composition (for species at >0.5wt%):
		O, Na, Mg, Si, S, Fe (only qualitative data)

b. isotopic composition:	
		O: 	About 3600 O-rich particles in large crater analyzed;
			no signatures from presolar O-rich grains; 
		C, N: 	About 440 C- and N-rich particles in large crater analyzed;
			15N = +451 ± 7 ‰
			13C = -25 ± 1 ‰
			(averages, normalized to foil contamination);
			no signatures from presolar C-rich grains
		S: 	About 550 S-rich particles in large crater analyzed;
			no signatures from presolar S-rich grains

c. size: 140 m (large crater); 0.1-1.7 µm (35 small craters identified in 1.6 mm2)
	d. mineral associations: n.m.

Contaminant phases identified (including melted aerogel):

Additional Notes: (paste sample image and /or EDS spectrum in JPEG format here if available)

SEM pictures of selected submicrometer-sized impact craters (upper row) and the large crater (left).