C2009,11,71

PICTURE HERE

C2115,23,21 keystone.

# Text boxes

Aliases:  18apr06

Track Characteristics

Type: small off-normal whisker track

Length: ~223 μm

Deepest particle diameter < 3 μm

Track History:

Prepared by Snead and Westphal at Berkeley

18apr06

Allocation History:

Keystone to Brownlee 19apr06

Images

Aerogel Cell:  hyperlink here

Aerogel Keystone:  hyperlink here

Track and Grains:

Microtomed samples:

Results

Terminal particle

Min/pet:

Bulk Chemistry:

Organics:

Isotopes:

Data Files:

Brownlee

brownlee 26may06 e-mail.pdf