NAME OF SAMPLE: TULE

TELEPHONE NUMBER: C2092,3,80

HISTORY: Aerogel piece containing bulb of track, but not track or TP, was sent from JSC in july 2006. The piece of aerogel was crushed by D. Brownlee and embedded in acrylic  and microtomed by G. Matrajt on 07/14/06.

MICROTOMY HISTORY: see excel sheet for details about # of sections per grid, thickness, and # of grids. Also, Au means gold grid; Cu means Cu grid, and // means parallel bar grid. The grid slot number corresponds to the slot in the grid box where the grid was originally stored.

Under comments, you will find  OPTICAL infomation only. Good means good sections. Bad means bad sections but they may be good electronically. When the grid was sent out the name of the person or institution holding the grid appears under comments. If it says 'washed with chloroform” it means that

the embedding medium was removed with chloroform vapors. If it says HF-etched, it means that the silicates were etched with HF vapors. If it says TEM, it means that the grid was surveyed and analyzed with an electron beam an could be possibly dammaged. For JSC,  the grid was removed from the grid box and placed in a mini-vial for shipping.

COMPOSITION DETERMINED WITH TEM by D. Joswiak and/or G. Matrajt:  There is not TP, juts pieces of particles that were found on the bulb of the track. Most of these pieces are melted aerogel. A ~ 3 um enstatite (with variable Cr, Mn and Al) was found surrounded by melt. Some carbon was also found.

SHIPPING INFORMATION:

Total number of grids sent: 7

Potted butt:  not sent

Particle in potted butt: small fragments still present.

Potted butt coated for SEM analysis: no