NAME OF SAMPLE: TARA

TELEPHONE NUMBER: C2004-T4 or  C2044,0,38. Track # 38. This is a track with two Tps.

HISTORY: Keystone prepared and sent  by A. Westphal. Track was crushed by D. Brownlee and embedded in acrylic  and microtomed by G. Matrajt on 06/01/06.

MICROTOMY HISTORY: see excel sheet for details about # of sections per grid, thickness, and # of grids. Also, Au means gold grid; Cu means Cu grid, and // means parallel bar grid. The grid slot number corresponds to the slot in the grid box where the grid was originally stored.

Under comments, you will find  OPTICAL infomation only. Good means good sections. Bad means bad sections but they may be good electronically. When the grid was sent out the name of the person or institution holding the grid appears under comments. If it says 'washed with chloroform” it means that

the embedding medium was removed with chloroform vapors. If it says HF-etched, it means that the silicates were etched with HF vapors. If it says TEM, it means that the grid was surveyed and analyzed with an electron beam an could be possibly dammaged. For JSC,  the grid was removed from the grid box and placed in a mini-vial for shipping.

COMPOSITION DETERMINED WITH TEM by D. Joswiak and/or G. Matrajt: Tp#1: largely aerogel melt + Fe Ni metal beads and a smaller region of bulk silicate glass (Fe+Mg+Al+Ca). Tp#2: is kamacite + small Fe oxide xtals on edge.

SHIPPING INFORMATION:

Total number of grids sent: 14

Potted butt: sent

Particle in potted butt: not visible optically but might have small fragments still present.

Potted butt coated for SEM analysis: no