NAME OF SAMPLE: PUKI-E,  debris of tiny particles around the field of fragment # 14. The debris have been named 101-108.

TELEPHONE NUMBER: Unknown. Track # 77. This is a track with one terminal particle and multiple fragments that made side tracks. Fragments were mounted sometimes individually and some times by groups in the same potted butt.

HISTORY: Keystone prepared and sent  by A. Westphal. Track was crushed by D. Brownlee and embedded in acrylic. Then the piece containing the debris around fragment # 14 was cut out and mounted over a potted butt  and microtomed by G. Matrajt on 07/18/07. It's called  PUKI-E. So, this potted butt contains tiny particles that were found around fragment # 14.

STATUS OF THE TRACK: the remaining of the track is in the UW clean room. Work is in progress as several fragments are still to be mounted.

MICROTOMY HISTORY: see excel sheet for details about # of sections per grid, thickness, and # of grids. Also, Au means gold grid; Cu means Cu grid, and // means parallel bar grid. The grid slot number corresponds to the slot in the grid box where the grid was originally stored.

Under comments, you will find  OPTICAL infomation only. Good means good sections. Bad means bad sections but they may be good electronically. When the grid was sent out the name of the person or institution holding the grid appears under comments. If it says 'washed with chloroform” it means that

the embedding medium was removed with chloroform vapors. If it says HF-etched, it means that the silicates were etched with HF vapors. If it says TEM, it means that the grid was surveyed and analyzed with an electron beam an could be possibly dammaged. If it says FTIR, it means it was surveyed with a Fourier-Transformed InfraRed by S. Bajt.  For JSC,  the grid was removed from the grid box and placed in a mini-vial for shipping.

COMPOSITION DETERMINED WITH TEM by D. Joswiak and/or G. Matrajt: not determined yet.

SHIPPING INFORMATION:

Total number of grids sent: 12

Potted butt: sent

Particle in potted butt:  small fragments still present.

Potted butt coated for SEM analysis: NO