Cell I1017

Track I1

Images

Level 2 – I1017.jpg

I1017A.jpg (Post Keystone)

Track and Grains:  N/A

Level 3:  N/A

Microtomed samples:  N/A

Track History:  Cell I1017 has been scanned via the Stardust@Home Project and selected as a candidate tile containing a track.  Track I1 is the first track removed from the Interstellar Tray and is classified as a high-angle track, meaning it may be “secondary” in nature (i.e., the projectile forming this track may have been ejecta from a particle impact somewhere o the spacecraft).

Discovered by Michael Hershberg

Extracted 12 feb 08
Analyzed at Brenker/ESRF by XRF.
Went to Flynn/NSLS, not analyzed by FTIR
Went to Westphal/UCB (SSL + ALS) 
Analyzed at ALS 1.4.3, FTIR (Bechtel) on 09Apr08
Removed from fork in plastic box with feed-throughs
Mounted in Si3N4 window sandwich
Analyzed at ALS 11.0.2 (Tyliszczak/Westphal)
Analyzed at ALS 1.4.3, FTIR (Bechtel) on 07May08

Track Characteristics:

Type: Type A Carrot

Length / Depth: ?

Grain diameters:?

Allocation History

Results

Track: No Data.

Data Files:

Analysis Summary
XRF: analysis shows terminal particles contain significant potassium, calcium, titanium, iron, zinc and cerium.

STXM: STXM analysis found magnesium, cerium, aluminum and zinc in the 2 µm terminal particle and in smaller fragments along the 300 µm track.

Aerogel was too thick for iron analysis, but no nickel detected.

No sodium found in track fragments

FTIR: Effects of the XRF analysis are visible in multiple bands of FTIR map (CH3, CH2, OH, C=O, amide).

Aerogel density is 18 mg/cm3 measured by STXM