Cell I1029

Track I10

Images

Level 2 – I1029.jpg

Track and Grains:  N/A

Level 3:  N/A

Microtomed samples:  N/A

Track History:  Cell I1029 has been scanned via the Stardust@Home Project and selected as a candidate tile containing a track.

Extracted 30Apr08 from fourth 9 o’clock swarm 5/3/08:

Went to Westphal/UCB
Removed from fork in plastic box with feed-throughs
Mounted in Si3N4 window sandwich
5/3/08: Analyzed at ALS 11.0.2 (Tyliszczak/Westphal)
Analyzed at ALS 1.4.3, FTIR (Bechtel) on 07May08

pikokeystone thickness is 70 µm

Track Characteristics:

Type: ?

Length / Depth: ?

Grain diameters:?

Allocation History

Results

Track:

Analysis Summary:

FTIR: analysis indicates large organic contamination, primarily in CH2 and amide regions. The contamination is distributed homogeneously throughout the keystone.

STXM: analysis found three 1µm particles in the picokeystone.  One particle contains sodium, possibly nickel, no iron, cerium, silicon.  2 other grains contain sodium, possibly weak aluminum, and silicon XANES like aerogel, no iron, magnesium, cerium

Carbon and nitrogen XANES on picokeystone.  Some nitrogen detected in fragment 2

Data Files: