Cell I1032

Track I11

Images

Level 2 – I1032.jpg

Track and Grains:  N/A

Level 3:  N/A

Microtomed samples:  N/A

Track History:  Cell I1032 has been scanned via the Stardust@Home Project and selected as a candidate tile containing a track.

1May08 Second IS candidate removed from tray

5/3/08: Went to Westphal/UCB
Removed from fork in plastic box with feed-throughs
Mounted in Si3N4 window sandwich
5/7/08: Analyzed at ALS 11.0.2 (Tyliszczak/Westphal)

Track Characteristics:

Type: ?

Length / Depth: ?

Grain diameters:?

Allocation History

Results

Track:

Analysis Summary:

ALS: This is an alumina grain embedded into the aerogel surface, and is probably not extraterrestrial

Data Files: