Sample Information Sheet

Sample ID: C2086N

Sample type (select one):

(6) foil

Type of analysis performed: 	SEM search for impact craters; C-, N-, and O-isotopic compositions (NanoSIMS) and EDX in large crater

State of sample pre-analysis: good

State of sample post-analysis (select one): partly consumed (large crater)

Minerals or other phases identified:

- a. elemental composition (for species at >0.5wt%):
		MgO (55.5%), SiO2 (41.8%), FeO (2.7%) (measured at NHM London)

b. isotopic composition:	
		O: 	About 2400 O-rich particles in large crater analyzed;

no signatures from presolar O-rich grains 
		C, N: 	About 900 C- and N-rich particles in large crater analyzed;
			15N = -11 ± 3 ‰
			13C = -21 ± 1 ‰
			(averages, normalized to foil contamination);
			no signatures from presolar C-rich grains
	c. size: 59 m (large crater); 0.1-0.9 µm (30 small craters identified in 0.5 mm2)
	d. mineral associations: Forsterite (97.5%) (measured at NHM London)

Contaminant phases identified (including melted aerogel):

Additional Notes: (paste sample image and /or EDS spectrum in JPEG format here if available)

SEM pictures of selceted submicrometer-sized impact craters.

SEM picture of large crater (from A. Kearsley, NHM London)